| Raychem Raychem Corporation 300 Constitution Drive, Menlo Park, CA 94025 | SPECIFICATION: RT-1800/13 THIS ISSUE: ISSUE 3 DATE: 7 SEPTEMBER 1989 REPLACES: ISSUE 2 |
| --- | --- |

THERMOFIT® HT-TMS®-CABLE MARKERS

HT-TMS-CM

Thermofit HT-TMS-Cable Markers are for use in marking applications up to 200°C, and are especially designed to identify cables, wire bundles, pipes and conduits. Cable Markers are made from radiation-crosslinked modified polyvinylidene fluoride, offering enhanced material properties, and ease of permanent marking.  They are also used in space applications where low outgassing is critical.

1.	SCOPE

This specification sheet, when used with RT-1800, defines the product characteristics and performance of the Raychem Thermofit HT-TMS-Cable Marker.

2.	REQUIREMENTS

2.1	MATERIAL

The markers shall be fabricated from irradiated, thermally-stabilized, modified polyvinylidene fluoride compound.  The material shall be homogeneous and essentially free from flaws, defects, bubbles, cracks, or inclusions.

2.2	COLOR

The markers shall be supplied in white, unless otherwise specified.

2.3	PROPERTIES

The markers shall meet the requirements of Table 2.

2.4	FORM

The markers shall be supplied as a continuous length of material on a carrier strip or bandolier suitable for automatic marking as described in Table 1.  Each marker can accommodate up to and including 22 characters per line, 12 pitch

TABLE 1

| PART NUMBER | FIGURE NUMBER | THICKNESS IN INCHES | NUMBER OF HOLES |
| --- | --- | --- | --- |
| HT-TMS-CM-1/4-4H | 3 | .020 | 4 |
| HT-TMS-CM-1/2-4H | 4 | .020 | 4 |
| HT-TMS-CM-1/2-6H | 5 | .020 | 6 |

Figure 1	Figure 2

1/4 -inch size	1/2-inch size

All Dimensions Nominal in Inches

CONFIGURATION OF CARRIER

Figure 3	Figure 4

HT-TMS-CM-1/4-4H	HT-TMS-CM-1/2-4H

Figure 5

HT-TMS-CM- 1/2-6H

All Dimensions Nominal in Inches

3.	QUALITY ASSURANCE

3.1	Qualification Tests

Qualification tests are those performed on markers and marker material submitted for qualification as a satisfactory product and shall consist of all tests listed in this specification.

3.2	Acceptance Tests

Acceptance tests are those performed on markers submitted for acceptance under contract.  Acceptance tests shall consist of the following:  dimensions, heat shock and print performance.

3.3	Test Specimens

Test specimens shall be individual HT-TMS-CM, detached from the carrier strip.  Where

RT-1800 is referenced as a test method, the term "marker" or "specimen" shall be understood to mean "HT-TMS-CM".

TABLE 2

Requirements

| PROPERTY | UNIT | REQUIREMENTS | TEST METHOD |
| --- | --- | --- | --- |
| PHYSICAL Dimensions | Inches | In accordance with Table 1 | Section 4.3.1.2 |
| Tensile Strength | psi | 3000 minimum | ASTM D 638 |
| Ultimate Elongation 1/8" wide die cut specimens | Percent | 200 minimum | Section 4.3.2.2 2 in. per min. |
| Specific Gravity | --- | 1.8 maximum | ASTM D 792 |
| Low Temperature Flexibility 4 hours at -55°C (-65°F) | --- | No cracking | Note 1 Section 4.3.5.2 |
| Heat Shock 4 hours at 275°C (527°F) Followed by test for: | --- | No dripping, flowing or cracking | Note 2 Section 4.3.6.2 |
| Print Performance (MIL-M-81531) | --- | legible | Section 4.3.10.2 |
| Heat Aging 168 hours at 225°C (437°F) Followed by test for: | --- | No cracking | Note 2 Section 4.3.7.2 |
| Print Performance (MIL-M-81531) | --- | legible | Section 4.3.10.2 |
| Print Performance (UL Subject 224) | Rubs | 50, Legible | Section 4.3.10 Section 4.3.10.1 Note 3 |
| (MIL-M-81531) | Rubs | 50, Legible | Section 4.3.10.2 |
| (MIL-STD-202) | Strokes | 50, Legible | Section 4.3.10.3 |
| Vacuum Outgassing TML (Total Mass Loss) | Percent | 1.0 maximum | Section 4.3.18 |
| VCM (Volatile Condensible Material) | Percent | 0.1 maximum | ASTM E 595 |
| CHEMICAL Corrosive Effect 16 hours at 200°C (392°F) | --- | No corrosion | ASTM D 2671 Procedure A Section 4.3.13.2 |
| Limiting Oxygen Index | --- | 40 minimum | ASTM D 2863 |
| Fungus Resistance | --- | Rating of 1 or less | ASTM G 21 |
| Water Absorption 24 hours at 23°C (73°F) | Percent | 0.5 maximum | ASTM D 570 |
| Fluid Resistance 24 hours at 23°C (75°F) JP-4 Fuel (MIL-T-5624) Skydrol 500* Hydraulic Fluid (MIL-H-5606) Aviation Gasoline (100/130) Lubricating Oil (MIL-L-7808) Salt Water (5% salt) Anti-Icing Fluid (MIL-A-8243) Followed by test for: | --- | --- | Note 4 |
| Print Performance (MIL-M-81531) | --- | legible | Section 4.3.10.2 |

* Trademark, Monsanto Company

Notes:	1.	In accordance with Section 4.3.5.2 except that specimens shall be bent 90 degrees  over a 1-inch mandrel.

2.	Specimens shall be bent 90 degrees over a 5/16-inch mandrel.

3.	Specimens shall be tied at each end to a 3/4-inch mandrel.

4.	Completely immerse three finished markers, marked in accordance with Section 4.3.10, and still on the carrier, in each fluid. The volume of the fluid shall be not less than 20 times that of the specimens.  After immersion, lightly wipe the specimens and allow to air dry for 30-60 minutes at room temperature.  Test the specimens for print performance in accordance with Section 4.3.10.2.